## Slide 1: Nanocrystalline Alloy Ribbons and Their Applications
Prof. Dr. Motoki Ohta
Global Research and Innovative Technology Center
(Professorship from Shimane University)

## Slide 2: About Me
Motoki Ohta
Affiliation
Senior Researcher: PROTERAL (Hitachi Metals)
Professor: Shimane University Next Generation Tatara Co-creation Center
Background
Academic degree: PhD. 2002 Tohoku University (Sendai Japan)
“Spin Fluctuation and Thermal Expansion Anomaly in Y6(Mn1-xFex)23 Compounds and Amorphous Alloys”
Work History:
  2002-05: Assistant Professor @ Tohoku University:
    Magnetics of solid-state metals
    Thermal expansion & Spin fluctuation (itinerant feature of spins)
  2005-now: Researcher @ Hitachi Metals (2013-15 Metglas):
    Development of rapid quenched soft magnetic materials such as nanocrystalline & amorphous ribbons
  2019-now: Professorship from Shimane University:
    Project Leader of the commercialization of amorphous motor
    Processing and characterization of Fe-based amorphous ribbon
My Lifework Research (relation with todays presentation)
Basically R&D person
Materials development, Soft magnetic properties
High Fe content nanocrystalline soft magnetic material (total citations: 979 google scholar)
  Most cited: APL 91 (2007) 062517. (citations: 152)
Pursuit of the origin of nanocrystallization and magnetic anisotropy in FINEMET®

## Slide 3: Contents
About PROTERIAL (Former Hitachi Metals)
Ideal Soft Magnetic Materials (SMMs) and
  Fe-based nanocrystalline alloy FINEMET®
SMMs in medium frequencies
  Development of High Fe content nanocrystalline alloys High Bs nanocrystalline alloy (Hi-Bs nano)
Applications of Hi-Bs nano
Remaining issues

## Slide 4: Corporate Summary
Date of Establishment
Capital
Representative
Number of Employees
Revenues
Number of Consolidated Subsidiaries
April 10, 1956
310 million yen （as of March 31, 2023）
Sean M. Stack - Representative Director, Chairman, President and CEO
Proterial, Ltd., Non-consolidated: 5,754 （as of end of March 2023)
Proterial Group, Consolidated: 26,496 （as of end of March 2023）
Proterial Group, Consolidated: 1,118.9 billion yen （FY2022）
Japan ２３, Overseas ３８, Total ６１（as of end of March 2023）
We were Hitachi Metals… Now we are PROTERIL

## Slide 5: Power Electronics Materials Business Unit
[Motor]
Our Advanced Soft Magnetic and Ceramic Materials Contribute to Energy Conservation and ICT innovations
We offer a long list of specialty materials and components; Metglas® amorphous metals, FINEMET® nanocrystalline materials and high-performance soft ferrites and ceramics.
Insulating substrate Si3N4
Nanocrystalline materials FINEMET®
(Ribbon, Core、Coil)
Ceramic Scintillator
Amorphous Magnetic Materials
for Motors
[Inverter]
[X-ray CT]
PROTERAL HP

## Slide 6: Magnetic Materials Business Unit
[Motor]
NEOMAX® brand, key material for industries
We boast an extensive magnet range, which includes NEOMAX® rare earth magnets and ferrite magnets, and provide our products across a wide range of fields, encompassing automobiles, electronics and home appliances. As pioneers in the field of magnetic materials, we take on the challenge of new materials and new production technologies, meeting our customers’ diverse needs and contributing to the creation of a more energy-efficient society.
Neodymium Magnets NEOMAX®
Ferrite Magnets NMFTM
PROTERAL HP

## Slide 7: Our Rapid Quenched Products
Holding Furnace
Water-cooled type Cast Roll
Ribbon Winder
Casting Control
Melting
Furnace
Nozzle
Rapid Quenching Cast Technology (Cooling Rate: ≥106℃/s )
Molten alloy is not crystallized to form alloy.
Alloy Name | Constituent Elements | Thickness | Grain Size | Induction | Core Loss
Grain Oriented Si Steel | Fe, Si | 230 μm | ～10 mm | ◎ | △
Fe-based Amorphous | Fe, Si, B | 25 μm | ー | ○ | ○
Nano-Crystalline Alloy | Fe, Si, B, Cu, Nb | 18 μm | ～10 nm | △ | ◎
Key Technology
Continuous
Rapid Quenching Cast
PROTERAL HP

## Slide 8: Amorphous Alloys for Transformers
Our main product for Rapid Quenching business
Amorphous Transformer*
Amorphous Alloy for Transformer “Metglas® 2605HB1M”
* Photo Credit: Hitachi Industrial Equipment System Co., Ltd.
PROTERAL HP
Notes: 8

## Slide 9: Major Bases (amorphous & nano)
■North America
Proterial America, Ltd.
Diehl Tool Steel, Inc.
Waupaca Foundry, Inc.
Ward Manufacturing, LLC
Metglas, Inc.
Proterial Cable America, Inc.
HC Queretaro, S.A. de C.V.
■Japan
Metglas Yasugi Works
Applied Components Dept.
Proterial Ferrite Electronics, Ltd.
PROTERAL HP
Yasugi, Shimane

## Slide 10: Products of Amorphous Alloy & “FINEMET®”
Application products using “FINEMET®”
Nano-Crystalline Soft Magnetic Material “FINEMET®”
Production capacity Amo & Nano total … １００kt/year (US&JP)
Item Amorphous alloy … width 142-213 mm, Thickness 0.025 mm
Nanocristillne alloy… W 50-85 mm, T 0.014-0.018 mm
1 spool = 100kg (17km)
1 m
PROTERAL HP
Notes: 10

## Slide 11
Ideal Soft Magnetic Materials (SMMs) and
  Fe-based nanocrystalline alloy FINEMET®

## Slide 12: Ideal SMMs
K: Mag-Cry anisotropy
λ: Magnetostriction
ρ: Resistivity
E: Young’s modulus
Bs (Ms): Induction
Intrinsic factors
(Structure,
Concertation）
H: Magn field
wdh: Size, dimension
(volume, cross section)
σ: Stress, Strain
Extrinsic factors
μ: Permeability
μi: Initial permeability
a: coefficient
Ideal SMMs→ zero K＋ zero l
Fe-Ni (Permalloy) Fe-Al-Si (Sendust)
Mn-Zn ferrite, Ni-Zn ferrite
Co-based amorphous alloy
non ideal soft magnetic materials are widely used if it is compatible with the usage.
Like amorphous ribbon in transformers which has High l
However, l is limiting its usage.
Tips
Relatively low Bs such as max 1 T or so
Motivation of developing
Material-derived factors
Controlling extrinsic factor to cancel the anti-factors
Fe-based nanocrystalline alloy, the FINEMET®
Notes: 軟磁性材料の要件として簡単に言ってしまえば
組成的・構造的にシンプルで当方的な材料が理想となります
軟磁性材料をめぐるエネルギーを整理するつもりで
頭に浮かんだことを線でたどって関連性を考えてみました。
かえって混乱するかもしれませんので
その場合はここは聞き流していただければと思います。
まず、材料が決まればそれに固有で決まるイントリンジックな数値があります
これがその例になります。
他方、外的因子すなわちエクストリンジックな値があります。
基本的に私たちが対象とする材料は、この両者の兼ね合いによって、その性能が再現されます。
私たちが対象とする軟磁性材料に求める要件として低損失が最重要項目ですが
損失には大きく分けて、3種類あります。
まずヒステリシス損失ですが、部材の形状が決まると反磁場が決まり、加工等で生じた応力と相まって、その材料内の磁区構造が決まります。
不可逆的磁化過程でよって B-Hループに履歴が生じ、1サイクルの損失分の損失が熱として奪われます。
この不可逆性の大きな原因になりうるのが、材料内のひずみです。
ひずみが内包された状態では磁歪定数を介して、透磁率の低下につながります。
ひずみにトラップされる形で、磁化反転起きにくくなることが、不可逆性の要因になります。
このような観点から軟磁性材料にとって低磁歪であることは非常に有利な条件となります。
また、多くの場合、加工や組み立てによって生じる軟磁気特性の劣化具合、すなわちビルディングファクターが生じますが、主たる要因は磁気弾性効果によることが多いです。
一方、この性質を逆手に取った磁歪を介した振動発電なども開発されており、悪いことばかりではないようです。
他方、この磁化過程のサイクルが繰り返される状態 すなわち交流磁場中において発生するのが渦電流損失であり、古典渦電流損失と異常渦電流損失に分類されます。
いずれも、動的な磁化過程で試料内の磁束が変化し続ける状態に対する抗力が起源で、磁束が変化するのを妨げる方向に磁束が発生し、それに伴い右ねじの法則で起電力が生じることで損失につながります。
特に異常渦電流損失は、従来といっても数十年前の話ですがの渦電流の概念では考えられていなかった磁化方向に直交する磁壁の移動に伴う損失で、原因不明だったために異常渦損と言われていました。
いずれの場合も電流を抑制することで損失を下げられるため、電気抵抗が高いことは有効と言えます。
形状的に渦損を抑えることは理にかなった方法と言えますが、例えば、薄く・小さくするのは渦損を抑えるためには有利に働くが ヒステリシス損失的には不利なので、目的や使用周波にあった形状選定は重要です。

## Slide 13: Magnetic Properties Comparison of Various Materials
103
104
105
106
0
0.5
1.0
1.5
2.0
2.5
Co-based Amorphous Alloy
Permalloy
Fe-based Amorphous Metglas®
Mn-Zn Ferrite
Fe-Al-Si Alloy
Si-Steel
Saturation Induction Bs (T)
Frequency=1 kHz
Downsizing
Nano-Crystalline Material “FINEMET®”
Permeability μri( kHz)
High Efficiency

## Slide 14
Bm=0.1T, Gap=0mm
Si-Fe (t=0.23mm)
FINEMET (t=0.018mm)
6.5% Si-Fe (t=0.1mm)
Transformer for high frequency
Cut core
Mobile phone
Shield sheet
Mn-Zn Ferrite
xEV
Noise filter for OBC,
Inverter, etc.
Wind and solar power
Train
Wound core
High efficiency
Reduction in size and weight
Main applications using FINEMET®
PROTERAL HP

## Slide 15: B-H loop Options
By controlling shape of B-H loop
Can be used for many purpose
Variety of Flavors
PROTERIAL HP, Catalog

## Slide 16: Example for PE ~High frequency transformers~
40 kVA 10 kHz High Frequency Transformer
● Transformer suitable for
high-power, high-frequency SW circuits
Metglas® 2605SA1
FINEMET®
F3CC Series
Mn-Zn Ferrite
CRGO (t=0.23mm)
6.5 % Si- Steel (t=0.1mm)
Bm=0.1 T
FINEMET®
FT-3L Ring core
Core Loss vs. Frequency
Frequency (kHz)
App ex:
EV, PHEV Quick charger,
Welding machines,
medical equipment
Other inverter applications
0.3 m
0.6m
0.4m
0.5m
Size comparison vs 40 kVA commercial
freq. trans.
Volume 約 1/20
Weight 約 1/30

## Slide 17: FINEMET & Metglas in EV&PHEV
～
Noise Filter
PFC Circuit
Boost Converter
Motor
Buttery
Boost Converter
Inverter
④Metglas® Reactor (Cut core)
2. FINEMET® Common Mode Choke
● Automotive charging circuit
/ Quick Charger
1. FINEMET® Common Mode Choke
②FINEMET® Transformer
Applications requires power density
PROTERAL HP

## Slide 18
SMMs in medium frequencies
  Development of High Fe content nanocrystalline alloys High Bs nanocrystalline alloy (Hi-Bs nano)

## Slide 19: Applications which requires higher Bs
Hc
Bs
H
Reactors
Motors
frequency
Hz
kHz
MHz
Neary full loop
Choose materials with a good balance of high Bs and low losses to obtain high power density
at the expense of the best low-loss performance
Applications that use B-H loops throughout
Medium frequency (sub kHz – tens kHz)
Output will be determined not only by the Bs, but also by frequency.
Higher the frequency, higher the core loss i. e it creates heat.
If the coefficient of core loss is low, it is easier to pull out power by increasing driving frequency.
PROTERAL HP

## Slide 20: Metallic SMMs on Bm vs. Hc map
Direction
low loss, high permeability
Coercivity : Hc (A/m)
1.0
1.5
100
101
Fe nanocrystalline alloys
(ex. Finemet® NanoparmTM)
Fe –amorphous alloys
0.5
Smaller / higher power
Operating magnetic flux density： Bm (T)
high Bm
low Hc
Bm: determined by Saturation magnetic flux density Bs
& iron loss
Si steels
Bm vs. Hc Tradeoff
Notes: This is a map of soft magnetic materials on Bm versus Hc plane
Here Bm stands for maximum operating flux density and Hc is coesevity
Bm are determined by saturation magnetic flux density Bs and iron loss
from this graph we can see Bm and Hc are tradeoff relation
what we want is mistrals go beyond this curve.

## Slide 21: Soft magnetic materials on the Bm vs. Hc map
low loss, high permeability
Coercivity : Hc (A/m)
1.0
1.5
100
101
Fe nanocrystalline alloys
(ex. Finemet®)
Fe –amorphous alloys
0.5
Smaller / higher power
Operating magnetic flux density： Bm (T)
Si steels
Lower Hc in crystalline system?
or
Higher Bs in
nano/random systems?
Two approaches
Fe crystal has higher Bs
random structure exhibits good SMM
Notes: so on the map
there is two way to go
One reducing Hc of Si steels
or
making Bs high of nano-scale random system such as amorphous or nanocrystalline alloy

## Slide 22: Concept of Materials Development
high Fe content nanocrystalline phase
High Bs & Low Hc
Soft magn. prop.
Amorphous
or Nano
High Bs
↓
High Fe content
bcc Fe phase
High Bs Nanocrystalline alloy
Notes: so we aimed overwrapped concept of these two
high Fe content in nanocrystalline phase to realize High Bs and Low Hc at same time

## Slide 23: Characters of FINEMET® composition
Fe: source of magnetic moments
Nb: high number density of seeds & suppresses grain growth
(at.%)
Composition of FINEMET® alloy
Fe73~75Cu0.8~1.0Nb2.6~3.0Si13~16B6~9
Low Fe, relatively high Nb ⇒ Low Bs
Y. Yoshizawa, et. al.: Mater. Sci. Eng., A181/A182 (1994) 871-875.
Notes: Let’s see characters of this composition
it has relatively low Fe content and high X elements
which makes Bs low

## Slide 24: Annealing process of FINEMET®
Annealing process
As-Q
Nb: Suppress Cu migration
Helps high number density of grain nucleation
Nb: Enhance thermal stability of residual amorphous phase
K. Hono, et al, Acta Mater. 47 (1999) 997.
bcc Fe-Si
（Fe-Cu-Nb-Si-B)
Suppress Grain growth
Nb = indispensable element
Cu cluster
Primary crystals
grain growth
Our purpose: Zero magnetostriction
Fe-Si has negative magnetostriction
Residual amorphous phase has positive one
The balance of volume fraction of each phase
is important
Notes: conventional nanocrystalline alloys are casted as an amorphous phase
at the early stage of annealing process, Cu clustering happens and these becomes seeds of primary crystals
they grow in the higher temperature
in this process Nb or Zr, I call X elements in this presentation, plays crucial roles
at the Cu clustering, X elements suppress the move of Cu atoms which help remaining high number density of seeds
and in the grain growth temperature, they go into residual amorphous phase and make it thermally stable
These X elements are necessary

## Slide 25: Adopting Quick Anneal
Fe80~83Cu0.8~1.0Nb0.0~1.0Si0~7B12~15 (M = Nb, Mo …)
Roles of Nb elements
→ substituted by Quick Anneal
(at.%)
Fe73~75Cu0.8~1.0Nb2.6~3.0Si13~16B6~9
increase
decrease
Composition of FINEMET® alloy
Approach 2. Rob migration time of Cu atoms
at the expense of low magnetostriction, aim high Bs
(flash anneal)
Notes: So we made some modify of composition
increase Fe and decrease X elements like this
And substitute the roles of X element by Quick anneal

## Slide 26: Cu clustering in Normal Annealing in new composition
Slowly passing Clustering temp. range
Cu atom can move long distance
clusters grow larger =
coarsening and decrease of number
Lack of seeds → grains grow large
As-Q
Clustering Temp. range
Cu migration
crystallization Temp.
Cu atom
Notes: when normal anneal has been applied for that composition
it passes clustering temperature range slowly
then Cu can move long distance
cluster grow and they become larger and number density decreases
due to lack of seeds grains becomes large

## Slide 27: Cu clustering in Quick Annealing
passes clustering temp. instantly
Reaches crystallization temp.
before number density of clusters becomes low
As-Q
High number density of seeds remains → fine nanocrystalline phase
Clustering Temp. range
Cu migration
crystallization temp.
Notes: however by applying quick anneal
that is passing the clustering temperature fast
there is not enough time for Cu to travel long distance
and Cu clusters remains small and high number density
Thanks to high number density of seeds grains become small and uniform

## Slide 28: B-H loops of NA and QA ribbons
QA: Quick Anneal
NA: Normal anneal
Hc < 3 A/m
Hc > 100 A/m
Low Nb, but high Bs & low Hc
QA
M. Ohta, Y. Yoshizawa, JMMM 321 (2009) 2220–2224.
Notes: we can see good soft magnetic properties
such as low Hc of 3 A/m with having Bs of 1.75 T

## Slide 29: Position of developed high Bs nano alloys
1.0
1.5
100
101
0.5
Quick Anneal type
Primary Crystal type
Loss is 1/3 of Si-steels
Bs・Bm are 10% higher than Fe-AM
low loss, high permeability
Coercivity : Hc (A/m)
Fe nanocrystalline alloys
(ex. Finemet®)
Fe –amorphous alloys
Smaller / higher power
Operating magnetic flux density： Bm (T)
Si steels
Quick annealing type may be suitable for industrial products
If we can solve the processing issues
Notes: The developed materials can be put on the map like this
it exhibits one third of core loss of Si-Steel and 10% higher Bm than Fe-amorphous alloy
it seems quick anneal type alloy is suitable for industrial products, if we can solve the processing issues

## Slide 30
Applications of Hi-Bs nano
  Block core for a reactor
  Motors

## Slide 31: Core types
Block core
(laminated)
Toroidal core
thickness of lamination
wound ribbon
http://kuretake-denko.co.jp/pages/core_shurui/TOR.html
Affects annealing
We cannot apply quick anneal to cores
Quick anneal first
then form the core
We want to search application field for this material.
Easy to implement and easy to adapt to various applications
Notes: These are the possible shape of applications
one, block cores may be impregnated
and toroidal core
but first of all, we found issue of annealing coursed by lamination thickness

## Slide 32: Soft magnetic properties block cores
83
63
19
35
laminate single strips
mold (impregnation)
cutting/Grinding/Etching
Block
Form a circuit by 4 blocks
HBN core
M. Ohta et al.: IEEE. Trans. Mag. (2018).
continuous Quick (flash) anneal
spool
Notes: so we prepared cores
first laminate single strips
mold it by resin
cutting grinding and etching had carried out
and we got a block
made core by 4 blocks

## Slide 33: Soft magnetic properties block cores
Hi-Bs nano core shows high B2000
 | B2k (T) | Bs (T) | B2k/Bs | ls (10-6)
HBN | 1.73 | 1.75 | 99% | 14
Fe-AM | 1.50 | 1.57 | 96% | 27
Better saturation behavior in HBN.
Hi-Bs nano can handle 10~15% larger DC superposition current
M. Ohta et al.: IEEE. Trans. Mag. (2018).
Notes: this is the B-H loop of High Bs nano block core
here we compered with that of Fe-based amorphous core
as we can see in the table
High Bs nano core shows more than 15% higher B at two thousand ampere per meter
that is because high Bs nano shows better saturation behavior of B
it reaches 99% of Bs at two thousand ampere per meter where Fe amorphous core is 96%

## Slide 34: Soft magnetic properties block cores
Chart: f (kHz)
| 2 | 5 | 10 | 16 | 20 | 30
200(AMCC) | 1.5892 | 5.0931 | 12.7062 | 32.3968 | 56.9421
200(125) | 1.3384 | 3.7072 | 8.5797 | 15.5892
 | HBN core | Fe-AM core
P2/10k (W/kg) | 8.5 | 12.7
P1/20k (W/kg) | 5.4 | 7.7
2/3 of core loss of Fe-AM
Amorphous core is recognized as a sufficiently low-loss material
M. Ohta et al.: IEEE. Trans. Mag. (2018).
Notes: and here is the core loss
it shows two thirds of Fe based amorphous core

## Slide 35: loss separation of block cores
Ptotal= Ph+Pe+Pex
Ph∝f 1
Pe∝f 2
Pex∝f 1.5
P = af + cf 2+ bf 1.5
P/f = a + cf + bf 0.5
Contribution of excess eddy current loss is dominant in medium f
conventional plot: liner = eddy current
b is strongly depending on pinning of domain wall
High Bs nano can be used in higher frequency
c : negligibly small
M. Ohta et al.: IEEE. Trans. Mag. (2018).
Notes: when we do loss separation we can find big difference
the top graph is well known P per f versus f graph
and the bottom one is P per f versus f to the power of 0.5th graph
we see straight relation in bottom one
that means the contribution of excess or in other words anomalous eddy current loss is dominant in these frequencies

## Slide 36
Comparison of core materials in Φ50mm motor
SPEC
item | value
Stator | Φ50 mm
Rotor | Φ31.4 mm
Gap | 0.3 mm
Thickness | 50 mm
Stator core Material | Amorphous (HB1M: PROERIAL)* Hi Bs Nano (PROTERIAL) Si-steel (35H300: Nippon Steel)
Output | 30 W (at 1000rpm) 300 W (at 10000rpm)
Voltage | Max. 200V
Current | Max. 3A
Motor
Cross section
*result from Shimane Univ
Stator
Rotor
Permanent
magnet
Coil

## Slide 37: Result from Simulation
Amorphous, High Bs Nano:
@10000rpm(1333Hz) 85% lower core loss than Si-steel core
Similar torque
Contour Diagram
RPM | Core material | Torq (Nm) | Coil loss (W) | Core loss (W) | Total loss (W)
1000 min-1 (133Hz) | Amorphous* | 1.03 | 3.06 | 0.147 | 3.207
 | Hi Bs Nano | 1.03 | 3.06 | 0.137 | 3.197
 | Si-steel | 1.02 | 3.06 | 1.175 | 4.235
10000 min-1 (1333Hz) | Amorphous* | 1.03 | 3.06 | 2.917 | 5.977
 | Hi Bs Nano | 1.03 | 3.06 | 3.308 | 6.368
 | Si-steel | 1.02 | 3.06 | 39.82 | 42.88
Analysis (@3.2 A)
Core
1/14
Total
85%↓
2.2T
0
1.1T
Core
1/8
Total
25%↓
*result from Shimane Univ
Very meaningful difference can be expected!

## Slide 38: Actual Measurement Results
Chart: Torque [Nm]
| 2.4516630000000001E-2 | 4.9033260000000002E-2 | 9.8066520000000004E-2 | 0.14709977999999999 | 0.19613304000000001 | 0.2451663 | 0.29419955999999997 | 0.34323282000000005 | 0.39226608000000002
高Bsナノ結晶機(16P) | 72.1752 | 84.1762 | 88.5847 | 87.2409 | 87.8003 | 88.9244 | 86.3329 | 81.676 | 79.5205
アモルファス機(16P) | 22.1325 | 68.5243 | 81.5903 | 83.9012 | 80.7915 | 79.0773 | 77.9252 | 73.3536 | 71.1466 | 69.4511
電磁鋼板機(16P) | 16.3887 | 49.4245 | 64.1844 | 75.2617 | 79.1555 | 79.9194 | 79.2166 | 78.6178 | 79.4341 | 76.681
Chart: RPM
| 498 | 1005 | 1500 | 2005 | 2500 | 3000 | 3510 | 4010 | 4500 | 5010 | 5500 | 6000 | 10000
高Bsナノ結晶16P | 0.067796 | 0.16839 | 0.28274 | 0.41993 | 0.54978 | 0.69115 | 0.73513 | 0.88185 | 1.0367 | 1.2592 | 1.4975 | 1.7593 | 3.9103
アモルファス16P | 0.1 | 0.2 | 0.3 | 0.5 | 0.6 | 0.7 | 1 | 1.1 | 1.3 | 1.6 | 1.7 | 1.9 | 4
電磁鋼板16P | 0.2 | 0.6 | 1.1 | 1.6 | 2.2 | 2.8 | 3.7 | 4.3 | 5.2 | 6 | 6.9 | 7.9 | 18.4
No-load loss: equivalent to Amorphous and Hi-Bs nano teeth
In the light-load: efficiency of Amo/Hi-Bs nano…significant improvement
In the high-load: the proportion of coil loss increases, so the difference with Si-steel core decreases, and eventually the efficiency is reversed
There is an optimal design point for utilization
Significant improve of efficiency
Si-Steel
Amorphous*
Hi Bs Nano
Si-Steel
Amorphous*
Hi Bs Nano
@6000 rpm

## Slide 39: Issues of amorphous ribbon production
No problem in shearing process
Otherwise
Thin & hard … requires more processes than thick & soft materials
Punched (stamped) amorphous ribbon as a stator shape
But don’t forget that “thin” will lead to low eddy current loss in high freq.
Now we are trying to keep the number of strokes down in punching process
Go simpler shape!
*nanocrystalline ribbons are also casted as amorphous phase
Shearing is easy!

## Slide 40: Radial Gap Motor
Si-steel (gray color)
Amorphous（pink）
Ref: All Si-steel
①Teeth of stator
(Amorphous)
The models, Cross section of ¼ of Motor
Rotor
Stator
Si-steel
High Bs nano（pink）
Contents | IPM Motor
Power | 22kW(6000 rpm, 35 N･m) Max：66kW(7000 rpm，90 N･m)
Torque | 90 N･m
RPM | 20000r/min
Size | φ215×50mm（1.8L）
Weight | 13.6kg
Efficiency | 96.0%（Calculated value）
SPEC
Si-steel
Teeth of stator
(Hi Bs Nano)
This simple shape can be prepared by shearing
Yuji Enomoto et .al: IEEJ Transactions on Industry Applications 143 (2022) pp.330–336

## Slide 41: ■No-load loss
Chart: RPM
| 0 | 522 | 1001 | 1501 | 1982 | 2498 | 2999 | 3501 | 4006 | 4500 | 5000 | 5500 | 6000 | 6500 | 7000 | 7500 | 8000
電磁鋼板機 | 0 | 7.4172 | 17.071 | 25.3506 | 38.4791 | 55.7187 | 73.845 | 89.4713 | 104.1183 | 130.3221 | 156.0864 | 184.3068 | 217.3982 | 250.4897 | 282.2197 | 318.8717 | 354.3717
アモルファスティース | 0 | 7.4172 | 14.9892 | 23.7661 | 34.5057 | 44.4703 | 56.3225 | 71.798 | 83.6292 | 99.1581 | 114.8462 | 138.806 | 160.8495 | 180.3798 | 205.2507 | 231.6925 | 261.3805
高Bsナノ結晶ティース | 0 | 6.3879 | 16.441 | 26.8606 | 38.5369 | 51.0509 | 63.146 | 77.7021 | 93.41 | 111.2124 | 130.8997 | 150.9012 | 170.9026 | 191.9513 | 214.0472 | 237.1902 | 261.3805
Similar tendency
Yuji Enomoto et .al: IEEJ Transactions on Industry Applications 143 (2022) pp.330–336

## Slide 42: Current vs. Torque
Chart: Current I（Arms)
| 0 | 30 | 60 | 90 | 120 | 150 | 180 | 210 | 240
電磁鋼板機 | 0 | 9.3 | 21.9 | 36.8 | 52.2 | 66.7 | 79.2 | 92.1 | 103.2
アモルファスティース | 0 | 4.3 | 9.4 | 15.5 | 22.3 | 29.3 | 35.8 | 42.2 | 48.3 | 53.7 | 58.9 | 63.5 | 68.01 | 72.3 | 76.5 | 79.8 | 83.1
高Bsナノ結晶ティース | 0 | 11 | 24 | 38 | 51.1 | 63.2 | 74.1 | 84.2 | 93.4
*The result could be expected
Improvement of torque form amorphous
Si-Steel
Amorphous
Hi Bs Nano
Yuji Enomoto et .al: IEEJ Transactions on Industry Applications 143 (2022) pp.330–336

## Slide 43: Efficiency map (tested result)
93
94
95
96
Teeth amorphous
Teeth Hi Bs Nano
Higher efficiency in wide condition
・Si-steel ＜ Amorphous (teeth) ＜ High Bs nano (teeth)
＊… So far, the high Bs nano is the best
Si-steel
Torque
RPM
Highest efficiency
Yuji Enomoto et .al: IEEJ Transactions on Industry Applications 143 (2022) pp.330–336

## Slide 44
Remaining issues
  Recycling
  Punching processing

## Slide 45: Recycle Flow of AMT (2013～)
Recycle process
Retrieve AM core from AMDT
AM ribbon
Crushed AM core
Energy saving and Resource circulation
Wash and Dry
Crush and Screen
Discard AMDT
（産機）に掲載写真依頼中
AMDT core
AMDT
Capacity：50 MT/mo
（April, 2013～）
Recycle of Amorphous Transformer
Page 19

## Slide 46: Challenges for practical application
Material | Assumed production process and challenges | Countermeasure
 |  | ・Shearing method ex：Teeth core
 |  | ・Processing methods other than stamping ⇒developing
 |  | Shrinkage evaluation & distortion reduction New heat treatment method New piece adhesion method
New machining process
or Consider the usage
Challenges specific to Hi Bs nano
・Brittleness with crystallization
・Shrinkage
with crystallization
・High heating rate anneal
Anneal ribbon
↓ ↓
Lamination Shaping
↓ ↓
Shaping Lamination
Shaping
↓
Parts anneal
↓
Lamination
・Simpler Shape is easier
・ In-plane variation of contraction
・Handling issue
Material
Machining
Material
Machining

## Slide 47: Conclusion
In present speak, the magnetic properties and their applications of the nanocrystalline alloy ribbons were introduced. Developed materials can be one of the best candidate for next generation power electronics materials from several kHz to MHz.
FINEMET® is designed having zero K and zero l with high Bs owing to its nanocrystalline structure.
In high Bs nanocrystalline alloy, owing to high Fe content nanocrystalline structure, high Bs and low core loss can be realized simultaneously.