## Slide 1: IEEE PELS PELS Standards Overview of ETTC & IEC TC51 Standards for Magnetic Core Loss Testing
2023 August 17
Energy Innovation Center, Pittsburgh, PA

## Slide 2: Background Info on Working Groups (ETTC Vs IEC TC51)
Electronics Transformers Technical Committee (ETTC)
  Low Power: POUT ≤ 10 Kilo-watts
  Wide Frequency: (F > 1 Hz)
  Low Voltage: VWORKING <1 kV
IEC TC51- Magnetic components, ferrite and magnetic powder material
  Focus on higher frequencies: F ≥10 kHz
  Lower currents: I ≤ 125A
  Lower voltages: VWORKING <1 kV
  To prepare standards relating to:
    parts and components displaying magnetic properties and intended for electronics in a wide range of application areas, including telecommunications, computers, automotive, aircraft, audio-visual, digital camera, lighting, solar and wind power systems, welding, inductive heating, power conditioning (UPS), wireless charging, RFID and medical;
    parts associated with such components;
    measuring methods and tests, and specifications for transformers and inductors using such components;
    ferrite and magnetic powder materials.

## Slide 3: IEEE PELS ETTC / IEC TC51 (Active Standards Reference For Core Loss testing)
IEEE-393 Procedure for Testing Magnetic Cores
  Updated standard targeted for 2025Q1
IEC62024-3 ED1: High frequency inductive components – Electrical characteristics and measuring methods – Part 3: AC loss measured by sinusoidal wave of inductors for DC-to-DC converters
  Publication targeted for 2026Q1
IEC62044-3 ED2: Cores made of soft magnetic materials measuring methods – Part 3: Magnetic properties at high excitation levels
  ED2 to be published 2023Q3
IEC63300 Test methods for electrical and magnetic properties of magnetic cores
  To be published 2023Q3

## Slide 4: Standards for Magnetic Characterization (Material Vs Core Vs Component)
Material
  Comparisons Between Materials Not Structures
  Toroids of Fixed Physical Dimensions
  Sized to Avoid Impact of Physical Dimensions, etc.,
    For example, ratio of outside diameter to inside diameter
  Test Coils Turns and Conductor Size, Distribution of Winding
  Closed Magnetic Path
  Continuous Magnetic Path - No Discrete or Intrinsic Physical Air Gaps
Core
  Specific to Magnetic Material, Structure, Physical Dimensions, Gap
  Specific to Test Coils
    Agreed upon test coils
    Fill factors
    Leakage flux
  Impact of Discrete Physical Air Gaps, Intrinsic Air Gaps and Distributed Air Gaps

## Slide 5: Standards for Magnetic Characterization (Core Vs Component)
Core
  Specific to Magnetic Material, Structure, Physical Dimensions, Gap
  Specific to Test Coils
    Agreed upon test coils
    Fill factors
    Leakage flux
  Impact of Discrete Physical Air Gaps, Intrinsic Gaps and Distributed Air Gaps
Component
  Total Power Loss
  Specific to Component Fabrication
    In most cases different from test coils used for measurements of core parameters
  Coil Contribution On Power Loss Measurements
    Fringing
    Leakage flux
  Impact of discrete physical air gaps

## Slide 6: IEC 62044-3 ED1 (Magnetic properties at high excitation level)

## Slide 7: IEC 62024-3 ED1 (AC loss measured by sinusoidal wave of inductors for DC-DC Converters)

## Slide 8: IEC 63300 ED1 (Test methods for electrical and magnetic properties of magnetic powder cores)

## Slide 9: IEC 63300 ED1 (Test considerations for current measuring resistor)

## Slide 10: IEC 63300 ED1 (Test considerations for measurement equipment)

## Slide 11: IEEE 393 (Considerations for specific test methods)
Further categorize applicability of test for
  Research
  Design verification
  Product verification
  Reliability
  Manufacturing

## Slide 12: Curve Fits From Measurement Data Ranges (Some Typical Guidelines)
Frequency
  Target operating frequencies should be within range of measurement frequencies
    Including major harmonics
  If the raw measurements indicate deviation from linear on log-log plot
    Frequency exponent will be encompassing multiple frequency range behaviors
Flux Density – Volt Seconds – Peak to Peak Current
  Target operating conditions should be within range of measurement frequencies
  If the raw measurements indicate deviation from linear on ln-ln plot
    Frequency exponent will be encompassing multiple frequency range behaviors
Bias
  Minor Loops in non-linear region of major BH loop have different power loss than minor loops in linear region of major BH loop
Temperature
  Maintain constant temperature via
    Heat Sink – Verify that heat sink does not impact fringing effects
    Forced Air
= K

## Slide 13: Core Data eXchange Format (CDX) (Proposal in Process)
APEC 2023 Core Loss Measurements for Everyone – George Slama
Test Coil Details
  Turns
  Wire Size
  Winding technique

## Slide 14: Magnetic Characterization In General (Publicly Available Reference Information)
PSMA Magnetics Committee Technical Forum
  https://www.psma.com/technical-forums/magnetics
Workshop Presentations
  2016 Magnetics Workshop
  2017 Magnetics Workshop
  2018 Magnetics Workshop
  2019 Magnetics Workshop
  2020 Magnetics Workshop
  2021 Magnetics Workshop
  2022 Magnetics Workshop
Industry Session Presentations
  https://www.psma.com/technical-forums/magnetics/presentations
PSSMA Core Loss Studies
  https://www.psma.com/coreloss

## Slide 15: Summary
Measurement details are different for material testing, magnetic core testing and magnetic component testing
Magnetic core specifications must be specific to magnetic material, structure, physical dimensions and any intrinsic or introduced physical gap or distributed gap – must reference the test coil
Standard test procedures tend to try to be agnostic relative magnetic materials, magnetic structure and component assembly
  However, is circumstances warrant standards, recommended practices or guidelines can be developed for specific materials and structures
Since we are actively updating standards for core loss measurements (cores) and ac power loss measurements (components) – we need your inputs to guide the next releases

## Slide 16: ETTC/IEC TC51 (Reference Standards for Core Loss Testing)
Thank You